Characteristics:         Aqueous, aliphatic polyurethane dispersion based polyester.

Supplied as:             35% in water

Physical characteristics:   Appearance                          Translucence

Non-volatile constituent                35±1 %

Ionicity                          Non-ionic

PH value                            6.0 - 7.5

Viscosity                            ≤200 mPa·s

Mean particle size                     ≤100 nm

Organic solvent                       Free

Glass transition temperation Tg           -25℃

Elongation                           700-800%

Tensile strength                        20.1 Mpa

100%Modulus                         2.5 Mpa

Shear stability                         Good

Yellowing resistance                    Non- yellowing

Storage:                 The dispersion should be stored in a frost-free place in tightly sealed containers.  It contains no preservative.

Application:             Cost-effective. Its film has excellent elongation and elasticity, and excellent water resistance. It has good compatibility with cationic, anionic waterborne polyurethane and other cationic and anion waterborne resins.

The information and recommendations in this publication are to the best of our knowledge, information and belief accurate at the date of publication. Nothing herein is to be construed as a warranty, express or otherwise. In all cases, it is the responsibility of the users to determine the applicability of such information or suitability of any products for their own purposes. Statements or suggestions concerning possible use of our products are made without representation or warranty that any such is free of patent infringement and are not recommendations to infringe on any patent.