Characteristics:         Cationic, aqueous aliphatic polyurethane dispersion based on polyether.

Supplied as:             35% in water

Physical characteristics:   Appearance                          Translucence

Non-volatile constituent                35±1 %

Ionicity                          Cationic

PH value                            3.5- 5.5

Viscosity                            ≤200mPa·s

Mean particle size                     ≤100 nm

NMP, NEP, DMAC etc                 Free

Elongation                           900-1000%

Tensile strength                       5.1Mpa

Elasticity modulus (100% )              1.0Mpa

Shear stability                         good

Yellowing resistance                   non- yellowing

Storage:               The dispersion should be stored in a frost-free place in tightly sealed containers. It contains no preservative.

Application:           Cost-effective. Its film is soft, and mainly used in the leather primer and fabric processing etc.

The information and recommendations in this publication are to the best of our knowledge, information and belief accurate at the date of publication. Nothing herein is to be construed as a warranty, express or otherwise. In all cases, it is the responsibility of the users to determine the applicability of such information or suitability of any products for their own purposes. Statements or suggestions concerning possible use of our products are made without representation or warranty that any such is free of patent infringement and are not recommendations to infringe on any patent.