Characteristics:         Aqueous, aliphatic polyurethane dispersion based on polycarbonate.

Supplied as:             30% in water

Physical characteristics:   Appearance                          Translucence

Non-volatile constituent                30±1 %

Ionicity                          Cationic

PH value                            3.5- 5.5

Viscosity                            ≤100 mPa·s

Mean particle size                     ≤200 nm

NMP, NEP, DMAC                    Free

Elongation                           500%

Tensile strength                       14.3 Mpa

100%Modulus                        2.9 Mpa

Shear stability                        good

Dry/touch                            ≤30min

Dry/through                          ≤60min

Yellowing resistance                   non- yellowing

Storage:                 The dispersion should be stored in a frost-free place in tightly sealed containers.  It contains no preservative.

Application:              Its coating has medium hardness, excellent abrasion resistance, heat resistance, excellent water resistance and resistance to salt spray. Mainly used in metal surface treatment, fiberglass infiltration agent, and wood sealing primer, etc. It does not contain Restricted Substances and Declarable Substances in EU.

The information and recommendations in this publication are to the best of our knowledge, information and belief accurate at the date of publication. Nothing herein is to be construed as a warranty, express or otherwise. In all cases, it is the responsibility of the users to determine the applicability of such information or suitability of any products for their own purposes. Statements or suggestions concerning possible use of our products are made without representation or warranty that any such is free of patent infringement and are not recommendations to infringe on any patent.