Characteristics:     Aqueous, aliphatic polyurethane dispersion based on epoxy-modified Polycarbonate.

Supplied as:             30% in water

Physical characteristics:    Appearance                         Translucence

Non-volatile constituent                30±1 %

Ionicity                          Cationic

PH value                            3.5- 5.5

Viscosity                            ≤100 mPa·s

Mean particle size                     ≤200 nm

NMP, NEP, DMAC                    Free

Shore A Hardness (A)                   96

Shear stability                        good

Dry/touch                            ≤30min

Dry/through                          ≤60min

Yellowing resistance                   non- yellowing

Storage:                 The dispersion should be stored in a frost-free place in tightly sealed containers.  It contains no preservative.

Application:             The film has high hardness, excellent adhesion, wear resistance, acid and alkali resistance, water resistance, alcohol resistance and chemical resistance. Mainly used in metal surface treatment and wood sealing primer, etc.

The information and recommendations in this publication are to the best of our knowledge, information and belief accurate at the date of publication. Nothing herein is to be construed as a warranty, express or otherwise. In all cases, it is the responsibility of the users to determine the applicability of such information or suitability of any products for their own purposes. Statements or suggestions concerning possible use of our products are made without representation or warranty that any such is free of patent infringement and are not recommendations to infringe on any patent.